## Slide 1: Major Superstructure Inspection and Rating

## Slide 2: Wearing Surface
2
Bonded or fastened to the deck
In direct contact with the traffic
Not part of the “structural” deck
Purpose
  Protects the bridge deck
    traffic wear
    salt and water infiltration
  Provides a smooth wearing surface
  Provides skid resistance

## Slide 3
Wearing Surface
Types
  Asphalt
  Timber
    untreated
    treated
  Polymer membranes
  Concrete overlay
    silica fume
    high density
    latex modified
    other (Pyrament)
    fibre reinforced
  May have more than one type
    i.e. polymer membrane on concrete overlay

## Slide 4
Wearing Surface
Drive over deck at design or posted speed
Observe traffic crossing bridge
  Look for deflections or movement
  Listen for unusual noises
Look for defects common to the material
Look for debonding, loosening or loss of wearing surface
  Sound for debonding using hammer if suspected
Look for protruding nails in timber wearing surfaces
Look for loss of aggregate from polymer wearing surfaces or seal coats
Look for polishing of concrete overlays especially high density

## Slide 5
Wearing Surface
TT, TH and PT forms
PCS and PSR only
PCS, PSR, SG, SS, DT and CON forms

## Slide 6
Wearing Surface
Record or verify type
Record or verify
  Thickness
  Size (TH & PT only)
Record or verify the presence of Lateral Connection Problem (Y/N)
  PSR and PCS only
  Rate under girders
If no wearing surface, rating is for Deck Top
  TH, PT and TT only

## Slide 7
Wearing Surface
Record in Explanation of Condition location, severity and extent of
  Wear
  Scaling / raveling
  Cracks
  Debonding
  Wearing surface loss

## Slide 8
Wearing Surface
Rate according to existing condition and functionality
If wearing surface does not have sufficient skid resistance
  rate 4 or less
If wearing surface does not cover the entire deck (curb to curb)
  rate 4 or less
  rate 2 if traffic hazard
Exposed nails or other fasteners
  rate 4 or less
If speed has to be reduced due to potholes, missing planks, ruts or other deterioration
  rate 3

## Slide 9
Wearing Surface
Concrete Overlay Rating Guide
Crack definitions
  Hairlines <0.1 mm
  Narrow >0.1 mm and <0.3 mm
  Medium >0.3 mm and <1.0 mm
  Wide >1.0 mm

## Slide 10
Wearing Surface
Asphalt Pavement Condition Severity Guide

## Slide 11
Wearing Surface
Asphalt Pavement Condition Severity Guide (Part 2)

## Slide 12
Wearing Surface
Wearing Surface Rating Guide - ACP

## Slide 13
Wearing Surface
Wearing Surface Rating Guide
Polymer / Seal Coat

## Slide 14
Deck Drainage
Not included on TT, PT or TH forms
Poor drainage
  Common cause of deck deterioration
  May cause a hazard due to hydroplaning or icing
  Caused by inadequate design, construction or maintenance practices
  May affect other bridge elements
    superstructure
    substructure
    headslopes and sideslopes
Drainage system includes
  gutters, inlet boxes, scuppers, downpipes and catch basins
  drainage problems at deck joints
    sealed
    with plumbing
    non-watertight

## Slide 15
Deck Drainage
Deck Drain

## Slide 16
Deck Drainage

## Slide 17
Deck Drainage
Check for:
  plugging of inlet boxes, scuppers, downpipes and joint plumbing
  corrosion of metal components
  gouges, cracks, breaks or tears
    joint seals
  integrity of attachments and connections
    loose or missing bolts
    cracked or broken welds
    loose or open connections
  length of downpipes

## Slide 18
Deck Drainage
Check for:
  signs of ponding on the deck
  damage to the deck, curbs, girders and substructure
    staining (water and rebar corrosion)
    scaling
    freeze-thaw
    delaminations
    spalling
  erosion below downpipe

## Slide 19
Deck Drainage
Record or verify if drains or joint plumbing is clogged

## Slide 20
Deck Drainage
For timber decks or steel grating
  not on TT, TH & PT forms
water ponded on the deck rate 4 or less
water ponding is a hazard rate 2
drains leak or downpipes too short rate 4 or less
ponding, leakage or discharge causes significant deterioration of deck, curbs, girders or substructure rate 3 or less
erosion on sideslopes or headslopes from discharge rate 4 or less
Deck joint leakage causing damage - reduce rating

## Slide 21
Deck Top/Underside
Purpose
  Carries traffic loads
  Transfers loads to main structural members
  Can be in direct contact with traffic in the absence of a wearing surface
Types
  Cast in place concrete
  Precast concrete
  Timber
  Steel grate
Separate ratings for top and underside
  Except for PCS, rate underside with top and girders
May not be inspectable from the top
  Wearing surface
  Snow, ice or gravel

## Slide 22
Deck Top/Underside
Drive over deck at design or posted speed
Observe deck under traffic
  Listen for unusual noises
  Look for deflections or movement
Look over deck top and underside for problems with material
On concrete decks, sound suspect areas with a hammer to detect delaminations
  Birdbath locations
  Stained areas
  Badly cracked areas or adjacent to large cracks

## Slide 23
Deck Top/Underside
Deck Top rated separately except for PT, TH and TT where Wearing Surface / Deck Top combined
Applies to PT, TH and TT only
Applies to DT and SS only
Remainder applies to SG, PSR, CON, DT and SS

## Slide 24
Deck Top/Underside
Record or verify subdeck type and size for TH, PT& TT
Record or verify deck underside
  % defects for TH, PT & TT
  % stains for all others
Record if snow slots filled for DT & SS
Record location, severity and extent of
  Staining
  Scaling
  Cracks
  Delaminations
  Spalling

## Slide 25
Deck Top/Underside
Rate according to existing condition and functionality
Speed reduced due to deterioration
  rate 4 or less
Surface does not have sufficient skid resistance
  rate 4 or less
Steel grating
  connections are loose or broken rate 4 or less
  improper bearing or support on girders rate 4 or less
Timber
  minor splitting in non-adjacent planks - rate 5 or more
  any rot - rate 4 or less
  broken planks - rate 4 or less
  connections loose or broken - rate 4 or less

## Slide 26
Deck Underside Concrete Deck Rating Guide
Crack definitions
  Hairline <0.1 mm
  Narrow >0.1 mm and <0.3 mm
  Medium >0.3 mm and <1.0 mm
  Wide >1.0 mm

## Slide 27
Deck Underside
Concrete Staining Deck Rating Guide

## Slide 28
Concrete Girders
Purpose
  Receive the loads from the deck
  Transmit the loads to the substructure (through the bearings)
Three types
  Cast-in-place standard reinforced
  Standard reinforced precast
  Prestressed or post-tensioned precast

## Slide 29
Concrete Girders
Inspection is primarily visual, looking for
  Staining
  Scaling
  Cracks
  Delaminations
  Spalling
Observe girders under traffic and look for unusual deflections or movement
  Independent movement on laterally connected girders
Evidence of grout key or lateral connection failure
  Cracking or loss of grout in grout key
  Cracking in pavement
  Corrosion, or missing, loose or broken bolts at channel connectors
  staining on underside of keys

## Slide 30
Concrete Girders
Grout key failure

## Slide 31
Concrete Girders
On post-tensioned girders check end anchorage zones
Check for corrosion of prestressing or post-tensioning cables
  rust stains or cracking along sides of girders
  leakage onto ends of girders with staining from ends of cables
Cracking in end anchorage zone of prestressed girders
High load damage which breaks the concrete around the pre- or post-stressed cables
  Look for damaged or broken cables

## Slide 32
Concrete Girders
Record or verify the presence of cracking
  PCS, PSR & CON
  Not hairline/narrow flexural on PCS or CON
Record or verify the amount of spalling in %
  PCS and PSR
  Corrosion induced spalling on bottoms and sides over stirrups only
  % of total leg or girder length
Girder Detail Ratings on PCS forms only

## Slide 33
Concrete Girders
Record in Explanation of Condition location, severity and extent of
  Staining
  Scaling
  Cracks
  Delaminations
  Spalling
  Grout Key failure

## Slide 34
Reinforced Concrete Girder Rating
Applies to all plain reinforced concrete girders
  Not prestressed or post-tensioned
If curb girder only affected, can increase ratings by one
  Has lower load carrying function
  Does not apply to shear cracks

## Slide 35
Reinforced Concrete Girder Rating
Spalling or Longitudinal Cracking on Bottom of Legs
RATING DESCRIPTION
5 Medium crack & sound concrete - anchor zone
Wide crack/spall - other zones
4 Medium crack - anchor zone
Wide crack/spall sound concrete - other zones
4 Moderate section loss on main bars
or stirrup bends up to 10%
3 Wide cracks or spall with sound concrete
- anchor zone
2 Spall with unsound concrete - anchor
zone
2 Severe loss of section on main bars or
stirrup bends greater than 20%
*Increase rating one point for:
-PG and PA girders OR cracking limited to one leg
-Defects limited to curb girder only

## Slide 36
Reinforced Concrete Girder Rating
Shear Cracks
*Must be 60 degrees or less from horizontal
RATING DESCRIPTION
5 Narrow*
3 Medium*
2 Wide or growing*
*Reduce by one if wide longitudinal crack or spall in anchorage zone

## Slide 37
Reinforced Concrete Girder Rating
Other Defects
RATING DESCRIPTION
No effect Hairline or narrow flexural cracks
6 End diaphragm spall
Narrow map cracks
5 Top slab transverse crack
4 Medium or wide map cracking or
any map cracking with staining
4 Medium flex or narrow grout key cracks

## Slide 38
Reinforced Concrete Girder Rating
Other Defects
RATING DESCRIPTION
4 Small (150mm max) punchouts
3 Medium or wide grout key cracks
3 Other punchouts
3 Failed girder connectors
2 Wide flexural cracks
2 End diaphragm spall extending
into legs

## Slide 39
Reinforced Concrete Girder Rating
Typical Defects

## Slide 40
Prestressed Concrete Girder Rating
Applies to all prestressed and post-tensioned concrete girders
Reduce as needed to reflect condition & function
If curb girder only affected, can increase ratings by one
  Has lower load carrying function
  Does not apply to shear cracks

## Slide 41
Prestressed Concrete Girder Rating
RATING DESCRIPTION
4 Hairline cracks*
3 All other cracks*
3 Corrosion stains from strands
2 Cracks with corrosion in webs,
flanges or bottom of boxes
2 Any cracks that are growing
1 Cracks opening and closing or
with slippage
*Some cracks are acceptable and don’t affect rating

## Slide 42
Prestressed Concrete Girder Rating
Chamfer crack at girder ends: N=5, M/W=4
Longitudinal crack in bottom half of leg at girder ends: H/N= 5 M/W=4
Longitudinal crack underside of leg: H/N=5, M/W=4
Diagonal crack in web transition: =5

## Slide 43
Prestressed Concrete Girder Rating
Crack in girder end block
through transition zone
DBT Girders
Diagonal crack in end block area - rate 5
  Not extending into bottom 1/4 of girder
  No staining
  Reduce by 1 if into flange or thin web section

## Slide 44
Prestressed Concrete Girder Rating
SM,VS, SC, RD,
RM,PM,VM
Girders
Longitudinal crack on underside- rate 5
Longitudinal crack curb fascia- rate 5
Crack in fascia at pier connection- rate 5
Bottom diagonal crack in ends - rate 5
  Not longer than 0.5m from cap or seat
  No corrosion staining
  With corrosion staining- rate 3

## Slide 45
Diaphragms / Cross Frame
Purpose
  Distribute loads between girders
  Resist torsion forces
  Support the compression flange of the girder
Generally made out of the same material as the girder
  If not, usually steel
Rate according to condition and ability to function as designed
If diaphragms contribute to defects in the girder - rate 4 or less

## Slide 46
Steel Girder
Purpose
  Receive loads from the deck
  Transmit loads to the substructure
Two types
  Rolled beam
  Welded plate girders
Usually I-shaped
  Web
  Flanges
Each part of girder rated separately
Stiffeners
  Vertical at bearings & along span
  Horizontal in high bending stress areas
Cover plates
  Extra plates welded to flanges to increase capacity in high bending areas

## Slide 47
Steel Girder
Cracks
  Tension areas
  End of cover plates
  Stiffeners welded to bottom flange
  Re-entrant corners
  Changes in section
  Stiffener welds that cross the weld from flange to web
  Gouges, nicks, holes, collision damage
Buckling
  High stress areas such as at bearings

## Slide 48
Steel Girder
Alignment
  Twists, bows, bends, sags
Corrosion
  Top of bottom flange
  Around connections
  Under joints
Connections
  Loose or missing bolt or rivets
  Poorly fitted connections
  Misaligned bolt holes
  Deformed bolt holes
  Corrosion between plates
    warping of plates
Collision damage
  Grade separations

## Slide 49
Steel Girder
Notches or stress raisers in tension areas
  rate 4
If corrosion is causing a loss of section
  rate 4 or less
If any signs of distortion or misalignment
  rate 4 or less
If fatigue cracks or signs of distortion
  rate 4 or less
Elements with visible cracks
  rate 3 or less
Fatigue cracks in bottom flange extending into web
  rate 2 or less

## Slide 50
Steel Truss Members
Purpose of truss as a unit is to:
  Receive loads from deck
  Transmit loads to substructure (through bearings)
Three types of trusses
  Through
  Pony
  Deck
Member types are rated separately
Includes stringers and floor beams
Truss members in tension or compression
  Inspector must identify each
  Different concerns

## Slide 51
Steel Truss Members
Check alignment of trusses
  top chord alignment especially important because it is in compression
Check for wide or high load damage
  If any present, indicate “YES” and explain in Explanation of Condition
  Especially look at portal bracing and sway bracing
  Wide or high load damage will affect the rating of the member(s) damaged
    compression members rating are especially lowered by bends
    tension members by cracks or nicks
  Check connections and members adjacent to damaged member

## Slide 52
Steel Truss Members
Check each truss member in an orderly fashion
  On tension members or collision damaged members look for cracks at connections
    crack will most often be at first bolt hole on the member side
    light members with significant stress or stress reversal
  On compression members look for kinks or bows
  Look for welds or torch cuts
    crack prone
  Look for fatigue prone details
    sharp radius corners
    notches
    light members - especially with stress reversal
  Check which members govern load capacity
    Allowable Load on first page of form

## Slide 53
Steel Truss Members
Check each connection in an orderly fashion
  Loose or missing bolt or rivets
  poorly fitted connections
  misaligned bolt holes
  deformed bolt holes
  corrosion between plates
    warping of plates
Check for Corrosion
  Between Built up members
  Splash zone
  bottom chord, especially channel section

## Slide 54
Steel Truss Members
Corrosion causing a loss of section
  rate 4 or less
Distortion or misalignment on a tension member, no other defects - rate 5
Minor misalignment or damage to cross-bracing or portal - rate 5
Cracks in a tension member - rate 3 or less
Cracks in a compression member - rate 4 or less
Any fatigue cracks - rate 4 or less
  Cracks on bottom flange of floor beam or stringer extending into web - rate 2 or less