## Slide 1: MAINTENANCE & REHABILITATION OF CULVERTS

## Slide 2: Introduction
Widely used, started in 1950
  low cost alternative to bridges
  road system expansion in 60s and 70s
Installed by road builders
  local road authorities
  district forces (day labour)
Designs by Bridge Engineering then Regional Bridge staff, now consultants

## Slide 3: Technical Developments
Early history - many problems
  spectacular uplift failures
  undersized
  deformation and cracking
Need for quality backfill and compaction not recognized
Importance of end treatments

## Slide 4: Culvert Inspection
Regular inspection initiated in mid-80s
  before major problems or failures reported
inspection provides early detection of changes
most defects develop slowly
poor backfill often detected at first inspection
As constructed records shape at ends, quarterpoints and middle

## Slide 5
Include:
  Deformation
  Cracked seams
  Corrosion
Usual causes
  poor quality backfill
  frozen backfill
  poor compaction
  poorly prepared foundation
  corrosive environment
  piping
Structural Problems

## Slide 6: Structural Problems Deformation
Heaving floors
Bulging walls
Sagging roof
Severity measured as percent of design shape
Contributing factors
  backfill low shear strength
  culvert material low bending strength
  load carried in ring compression and soil-steel interaction

## Slide 7: Structural Problems Cracked Seams
Primary cause is deformations
  sometimes deformations small; 5%
  may occur at one or more seams
Contributing factors
  incorrect laps
  over torquing bolts
  improperly curved plate
Severity measure
  number of seams cracked
  location of seams
  remaining steel between cracks

## Slide 8: Structural Problems Corrosion
Corrosion
  electrochemical process that converts metal to natural state
Environmental requirements
  differences in potential
  electrolyte
  Oxygen
Corrosion types
  electrolytic
  galvanic
Severity measure
  percent rust pitting or perforation
  static potential
    950 mV galvanizing is good
    800 mV galvanizing is failing

## Slide 9: Waterside Corrosion on Culvert Floor

## Slide 10: Soilside Corrosion Damage

## Slide 11: Corrosion
Electrolytic corrosion
  caused by external stray currents
  other cathodic systems
  overhead power lines
Galvanic corrosion
  materials of different potential in an electrolyte
  impurities in metal
  differences in coatings
  surface defects
  moist soil good electrolyte
  generates own current

## Slide 12: Electrolytic Corrosion Mechanism

## Slide 13: Galvanic Corrosion Mechanism

## Slide 14: Repairs and Maintenance Methods
Monitoring
Strutting
Liners
Crack repairs
Cathodic protection

## Slide 15: Monitoring
Should be recommended sparingly – only when measurable (Section 13.9.1.2)
First option, low cost
  structure may stabilize – especially deflections
Provides ongoing record
  mark ends of cracks
  measure magnitude and location of deformations
  establish reference points
  photographs

## Slide 16: Strutting
Oldest, often cheapest method
Effective for extreme distress
Not suitable for drift and ice locations
Components
  vertical struts between sleepers
  cut to length, jacked in place
  timber or steel
Life ~25 years for timber – maybe longer for steel struts

## Slide 17: Timber Strut with Adjustable Turn-screw

## Slide 18: Strut Layout for Horizontal Ellipse Culvert

## Slide 19: Timber Strutting of Metal Culverts

## Slide 20: Installing Struts

## Slide 21: Completed Installation

## Slide 22: TT Struts and Braces

## Slide 23: Horizontal TT Strut

## Slide 24: Steel Struts

## Slide 25: Liners
Used when culvert cracked or corroded
Reduces hydraulic capacity
Increases velocities, back water
Not suitable for large deformations
Life 30 to 40 years

## Slide 26: Culvert Liners

## Slide 27: Liner Types
CSP culvert
  1.5m to 3.0m culverts
SPCSP
  larger than 3.0m culverts
  limited length
Tunnel liner
  large culverts and long length
Smooth wall pipe
  Usually <1.5 m diameter culverts

## Slide 28: Installing CSP Liner into Existing SPCSP Culvert

## Slide 29: Internal Bracing Installed Prior to Grouting

## Slide 30: Installing Steel Headwalls at Ends of Pipe to contain grout

## Slide 31: Grout / transit mix installed through holes cut into roof of original pipe.

## Slide 32: Winch at Outlet to pull new CSP liner into pipe

## Slide 33: Victaulic Connector for Concrete Pump

## Slide 34: Installing Tunnel Liner Inside Culvert

## Slide 35: Tunnel Liner Ready for Grouting

## Slide 36: Smooth Wall Steel Pipe Liner in CSP

## Slide 37: Concrete Floors
Repair severe perforations of invert
Reinforce cracked seams and sidewall deformation of arch culverts
Reduces hydraulic capacity

## Slide 38: Details of Concrete Floor for SPCSP Arch

## Slide 39: Reinforcing Steel Arrangement

## Slide 40: Concrete Floor Cast

## Slide 41: Finished Floor and Ponywall

## Slide 42: Reinforcing Steel Arrangement – Wire mesh

## Slide 43: Pouring Concrete Floor

## Slide 44: Ends of Pipe Tarped off to heat.

## Slide 45: Crack Repair Methods
stop drilling crack ends
welding cracks
reinforcing plates
  welded
  Bolted
reinforced concrete
  arch culverts
shotcrete

## Slide 46: Shotcrete Reinforcing
Preferred method for repairing cracks
Stiffens joint and transfers ring compression
sprayed over shear connectors and rebar
20-year life
Not suitable for:
  small cracks
  cracks on both sides
  severe corrosion
  large deformations

## Slide 47: Longitudinal Seam Reinforcing
Longitudinal Cross Section

## Slide 48: Pump and Mixer for Prewetting

## Slide 49: Detail of Reinforcing and Shear Connectors

## Slide 50: U-bracket Shear Connector

## Slide 51: Sandblast Equipment

## Slide 52: Heaters

## Slide 53: Reinforcing and Shear Connectors Ready for Shooting

## Slide 54: Shooting Concrete Mix

## Slide 55: Completed Crack Reinforcing Beam

## Slide 56: Completed Crack Reinforcing Beam

## Slide 57: Cathodic Protection
Prevents corrosion
  impressed uniform potential
  anode sacrificed to protect structure
  soil side corrosion only
System types
  impressed current system
  passive system

## Slide 58: Cathodic Protection
Impressed current system
  20 to 60 volts and 4 to 16 amps
  available power on site, 120/240 AC
  power supply, anode bed, electrolyte
  life - 15 to 25 years
Passive system
  dissimilar metals create current and potential
  many magnesium anodes sacrifice to protect structure
  1 to 2 amps and 1 to 2 volts
  life - 15 to 25 years

## Slide 59: Passive Cathodic Protection

## Slide 60: Culvert Cathodic Protection

## Slide 61: Anodes

## Slide 62: Anode Cross-section

## Slide 63: Downstream Restoration

## Slide 64: Jacking Culvert Under Highway

## Slide 65: Environment Controls - Siltation Fence

## Slide 66: Questions?