## Slide 1: CONCRETE PHYSICAL & MECHANICAL PROPERTIES

## Slide 2: Introduction
Composition
Physical Properties
Mechanical Properties
Defects & Deterioration

## Slide 3: COMPOSITION

## Slide 4: Composition
Portland Cement.
Aggregate.
Mixing Water.
Entrapped Air.
Admixtures.
Supplementary Cementing Materials.

## Slide 5: Proportions of Materials in Concrete
Coarse agg.
31 %
Fine agg.
28 %
Air
8 %
Water
18 %
Cementing
materials
15 %
Air-Entrained
Concrete
Non air-Entrained
Concrete
Mix 1
Mix 2
Mix 3
Mix 4
51 %
24 %
4 %
14 %
7 %
31 %
30 %
3 %
21 %
15 %
7 %
16 %
1 %
51 %
25 %

## Slide 6: Cross-section of Concrete

## Slide 7: Portland Cement
Invented in 18th century in England and was called Portland cement due to its similarity to Portland stone, a type of building stone commonly used.
Chemical compound which reacts with water (hydration) to form a stone like mass.
Tricalcium Silicate
Dicalcium Silicate
Water
Calcium Silica Hydrate
Calcium Hydroxide
C3S + C2S + H2O C3S2H2 + CH

## Slide 8: Portland Cement
73% Limestone
23% Clay
2% Iron
3% Sand
+
Gypsum
Grind
Heat
Clinker
Grind
Portland
Cement
1500°C

## Slide 9: Cement Manufacture

## Slide 10: Cement Manufacture

## Slide 11: Types of Cement
Type “GU” – General use.
Type “GUL” – 1st test project in Alberta in 2022 – 15% limestone added
Type “HE” – High early strength.
Type “MS” – Moderate sulfate resistance.
Type “HS” – High sulfate resistance.
Type “MH” – Moderate heat of hydration.
Type “LH” – Low heat of hydration.
Notes: Think of uses. HE precasters
MS/HS sea water, corrosive soils
MH/LH hydration. Not common for us. Maybe mass pours?

## Slide 12: Water
Potable water
Impurities cause
  abnormal set
  decreased strength
  volume change
  efflorescence
  corrosion of reinforcement

## Slide 13: Aggregate

## Slide 14: Characteristics of Aggregate
Clean & sound.
Abrasion resistance
Freeze & thaw resistance
Wetting & drying properties
Chemical stability
Alkali aggregate reactivity
Shape and surface texture
Aggregate grading

## Slide 15: Grading Limits
160
Percent Passing by Mass
Sieve sizes - nominal opening
315
630
1.25
2.5
5
10
20
40
56
20
40
60
80
100
µm
mm
Fine Aggregate
Coarse Aggregate

## Slide 16: Fineness Modulus
Fineness Modulus = 283/100 = 2.83
Sieve Size | Percentage Retained by Mass
10 mm | 0
5 mm | 2
2.5 mm | 15
1.25 mm | 35
630 µm | 55
315 µm | 79
160 µm | 97
Total | 283

## Slide 17: Air-Entrained Concrete
Improves freeze-thaw resistance
Improves workability
Finishes sooner
Reduces water
Reduces segregation and bleeding
Improves sulfate resistance
Entrained air content from 5% to 8%
Notes: Freeze-thaw

## Slide 18: Air-Entrained Concrete
Notes: Dark bubbles are air

## Slide 19: PHYSICAL PROPERTIES

## Slide 20: Physical Properties
Thermal expansion:
  Concrete 9.9 x 10-6/°C
  Steel 12.0 x 10-6/°C
Volume change due to moisture:
  Swelling
  Shrinkage

## Slide 21: Swelling/ Shrinkage
Swelling
Shrinkage
Time
Stored in water
Stored in air
Notes: Curing prevents shrinkage cracks.

## Slide 22: Water/Cement Ratio & Shrinkage of Paste
Drying Shrinkage 10-6
Age (Days)
7
28
90
180
270
360
0.8
1.6
2.4
3.2
W/C = 0.26
W/C = 0.45
W/C = 0.55
W/C = 0.65
Notes: More shrinkage in concretes with higher water-cement ratios

## Slide 23: MECHANICAL PROPERTIES

## Slide 24: Mechanical Properties
Strength
  Compressive (28 day – f’c)
  Tensile (10% of f’c)
  Shear (12% to 13% of f’c)
  Flexural (14% of f’c)
Abrasion resistance
Creep
Fire resistance
Durability
Permeability
Notes: Good compression. Not good tension. It cracks. This is why we add rebar

## Slide 25: Water/Cement Ratio vs. Strength
28 day compressive strength MPa
10
W/C Ratio
0.3
0.4
0.5
0.6
0.7
0.8
0.9
20
30
40
50
60
Non air-entrained concrete
Air-entrained concrete
Notes: As w/c increases. Strength decreases. However, workability.
Less air voids, higher strength. Freeze-thaw

## Slide 26: Effect of Curing on Strength
10
Age at Test Days
Compressive Strength MPa
20
30
40
50
In lab. air cured
In air after 7 days moist curing
In air after 28 days moist curing
Moist cured entire time
60
0
7
28
91
365

## Slide 27: Compressive Strength & Air Content
0
50
Compressive Strength @ 90 days - MPa
Air Content %
1
2
3
4
5
6
7
60
70
40
W/C Ratio
0.3
0.4
0.5
Notes: Class C and HPC w/c is 0.4
Air is 5-8

## Slide 28: Wear vs. Strength
Depth of Wear (mm)
Compressive Strength MPa
0
7
14
21
28
35
2.5
5.0
7.5
10
Notes: Basically describing relationship btwn low strength resulting in low surface durability & abrasion resistance. E.g. concrete bridge decks resisting tire and snowplow wear, concrete floors in culvert resisting rock/gravel abrasion. Durability increases as strength increases. Abrasion primarily affected by strength

## Slide 29: Concrete Strength & Creep
0
250
500
750
1000
1250
5
7.5
10
Creep Strain
Age (Days)
Concrete Strength 27.6 MPa
Concrete Strength 41.4 MPa
Notes: Higher strength means less creep.
Creep is deformation under constant (not changing) load

## Slide 30: Curing Method & Creep
0
50
100
150
200
300
Creep Deformation
Time after loading (Days)
250
350
7 days moist cured
Atmospheric steam cured
High-pressure steam cured
Notes: Better curing reduces creep.

## Slide 31: Age of Loading & Creep
0
250
500
750
1000
1250
5
7.5
10
Creep Strain
Age (Days)
Age of loading
28 days
90 days
180 days
Notes: Age of girders when they are installed affects creep

## Slide 32: Freeze/ Thaw Resistance, Air & W/C Ratio
W/C Ratio
0.3
0.4
0.5
0.6
0.7
0.8
0
1000
4000
3000
2000
0
1000
5000
3000
2000
4000
6000
Cycles of freezing & thawing to 25% loss in mass
Fog cured 14 days
Dried 76 days at 50% RH
Air entrained
concrete
Non-air entrained
concrete
Fog cured 28 days
No drying
Notes: Air entrainment helps for all cases.

## Slide 33: Permeability, W/C Ratio & Curing
Permeability cm/secx10-10
W/C Ratio
0.3
0.4
0.5
0.6
0.7
0.8
0
10
20
30
40
50
1 day moist, 90 days in air
7 days moist, 90 days in air
Non-air entrained concrete

## Slide 34: DEFECTS AND DETERIORATION

## Slide 35: Deterioration Stains
Notes: Water working its way through deck

## Slide 36: Staining, Efflorescence & Corrosion

## Slide 37: Deck Ponding

## Slide 38: Freeze – Thaw Damage

## Slide 39: Scaling Damage

## Slide 40: Light Scaling

## Slide 41: Medium Scaling

## Slide 42: Heavy Scaling

## Slide 43: Deteriorated Concrete Approach Slab
Notes: Flexible ACP at road side of approach slab often leads to deterioration of more rigid concrete wear surface of approach slab from vehicle impact ;loading. App slab is poured on granular bed and is prone to settlement if granular compaction is poor

## Slide 44: Surface Abrasion

## Slide 45: Sound Concrete Deck

## Slide 46: Sound Concrete Deck Underside

## Slide 47: Concrete Stress- Strain Relationship
Concrete Stress MPa
Concrete Strain
0.003
f’c
Strain =
L/L
L = 0.003x300 = 0.9 mm
Notes: crushing

## Slide 48: High – Performance Concrete
High strength.
High modulus of elasticity.
High abrasion resistance.
Low permeability and diffusion.
Resistance to chemical attack.
High resistance to frost.
Ease of placement

## Slide 49: Self – Compacting Concrete
Able to flow and consolidate on its own.
Must be cohesive to fill spaces without segregation.
Useful wherever placing is difficult.
SCC reduces the need for vibration.
It is based on increasing the amount of fine material without changing the water content.

## Slide 50: Shrinkage Cracks

## Slide 51: Map Cracking

## Slide 52: Flexural Cracks

## Slide 53: Construction Joint

## Slide 54: Corrosion Spalls & Pop – outs

## Slide 55: Corrosion Spall

## Slide 56: Corrosion Spall

## Slide 57: Alkali Aggregate Reaction

## Slide 58: High Load Impact

## Slide 59: High Load Damage

## Slide 60: Severe High Load Damage

## Slide 61: Questions?