## Slide 1: INSPECTION OF STEEL GIRDER BRIDGES

## Slide 2: Introduction
Topics Covered in this Presentation:
Bridge superstructure systems
Defects in steel members
Failure mechanics
Fatigue
Constrained Induced fracture (CIF)
Inspection
Inspection of Pin & Hanger

## Slide 3: Bridge Superstructure Systems

## Slide 4: Bridge Superstructure Systems
Rolled beams
  Manufactured from one piece of steel
  Webs are stocky, therefore no intermediate stiffeners.
  Used as simple spans with span length from 9 to 15 m
Rolled beams with cover plates
  Cover plates were added to increase the capacity
  Cover plates were welded or riveted to the flanges
  Welded cover plates created fatigue prone detail

## Slide 5: Bridge Superstructure Systems
Rolled Beam

## Slide 6: Bridge Superstructure Systems
Rolled Beam
with
Cover Plates

## Slide 7: Bridge Superstructure Systems
Steel Tub Girders

## Slide 8: Bridge Superstructure Systems
Built-up Girders
  Similar in appearance as rolled beams
  Custom fabricated, not produced in rolling mills
  Fabricated from thin plates, hence require stiffeners
  Older built-up girders were riveted, newer are welded plates
  Continuous girders can have spans over 150 m

## Slide 9: Bridge Superstructure Systems
Built-up
Girders

## Slide 10: Bridge Superstructure Systems
Girders with Pin and Hanger
  Analysis is simplified for a hinged structure
  It moves drainage away from piers
  Only one pin is required for rotation
  For translation and rotation, two pins and hanger are provided
Steel Arches
  Three types of arches: deck, through and tied
  Arch spans range from 300 to 500 m
Notes: Translation is a measure of how much a point in the structure has moved from its original position

## Slide 11: Bridge Superstructure Systems
Girder with
Pin & Hanger

## Slide 12: Bridge Superstructure Systems
Girder with
Pin

## Slide 13: Bridge Superstructure Systems
Steel Arch

## Slide 14: Bridge Superstructure Systems
Suspension Bridges
7. Trusses
  Through Truss
  Pony Truss
  Deck Truss

## Slide 15: Bridge Superstructure Systems
Suspension
Bridge

## Slide 16: Bridge Superstructure Systems
Through Truss

## Slide 17: Bridge Superstructure Systems
Pony Truss

## Slide 18: Bridge Superstructure Systems
Deck Truss

## Slide 19: Primary and Secondary Members
Primary Members for Bridge Systems 1 to 4
  Fabricated girders / Rolled beams
  Diaphragms for curved girders
  Pin and hanger
Secondary Members for Bridge Systems 1 to 4
  Diaphragms

## Slide 20: Primary and Secondary Members
Primary Members for Bridge System 7
  Trusses (chords, web members)
  Floor beams
  Stringers
Secondary Members for Bridge System 7
  Bracing

## Slide 21: Defects in Steel Members

## Slide 22: Steel Damage and Deterioration
Corrosion
  Environmental corrosion
  Stray current corrosion
  Stress corrosion
Cracking
  Fatigue
  Impact
  Excessive loading
  Deformation
    Excessive Loading
    Impact
    Heat Damage

## Slide 23: Steel Damage and Deterioration
Corrosion

## Slide 24: Steel Damage and Deterioration
Corrosion

## Slide 25: Steel Damage and Deterioration
Fatigue Crack

## Slide 26: Steel Damage and Deterioration
High Load Impact Damage

## Slide 27: Steel Damage and Deterioration
Impact Damage

## Slide 28: Steel Damage and Deterioration
90% failure of diagonal – wide load impact damage

## Slide 29: Steel Damage and Deterioration
Fire Damage

## Slide 30: Steel Damage and Deterioration
Fire Damage

## Slide 31: Steel Damage and Deterioration
Overload
Damage

## Slide 32: Fatigue & Fracture in Steel Members
Fatigue
  Tendency of a member to fail at a stress level below its yield stress when subjected to repeated loading
Fracture Critical Member (FCM)
  Member is in tension
  Member is non-redundant, its failure causes partial or total collapse of a structure

## Slide 33: Failure Mechanics
Describing the process by which a member fails when subjected to fatigue.

## Slide 34: Types of Fractures in Steel Members
Brittle Fracture
Ductile Fracture

## Slide 35: Fatigue Crack Categories
Fatigue failure process consists of three stages:
Crack initiation
Crack propagation
Fracture
Details and Defects
Out-of-plane Distortion
Fatigue Failure Process

## Slide 36: Factors Affecting Fatigue Crack Initiation (Details & Defects)
Plug welds
Tack welds
Material flaws
  External flaws (Surface scabs)
  Internal flaws (Non-metallic inclusions, Rolled in plate defects)
Weld flaws
  Non-visible flaws (IP welds, Porosity, Slag inclusions)
  Visible flaws (Undercut, Overlap)
Fabrication Flaws
  Cutting of plates, Holes, Coping

## Slide 37: Factors Affecting Fatigue Crack Initiation (Details & Defects)
Transportation & Erection Flaws
  Nicks
  Notches
  Indentation
In-Service Flaws
  Collision damage
  Improper heat straightening
  Torched or notched holes

## Slide 38: Plug Weld

## Slide 39: Tack Weld

## Slide 40: Material External Flaw

## Slide 41: Material Internal Flaw

## Slide 42: Incomplete Penetration Weld

## Slide 43: Incomplete Penetration Weld

## Slide 44: Weld Crack Due to Slag Inclusion

## Slide 45: Fillet Weld Draws
UNDERCUT
OVERLAP

## Slide 46: Improper Web Coping
Web Cope

## Slide 47: Correct Web Coping

## Slide 48: Torched Hole

## Slide 49: Torched Damage

## Slide 50: Factors Affecting Fatigue Crack Initiation (Out-of-plane Distortion)
STIFFENER
TOP FLANGE
WEB
WEB GAP

## Slide 51: Girder Differential Deflection
DIAPHRAGM
STIFFENER
DECK

## Slide 52: Girder Web Gap Distortion
WEB GAP
DISTORTION
TOP FLANGE
WEB
STIFFENER

## Slide 53: Girder Web Gap Distortion

## Slide 54: Factors Affecting Fatigue Crack Propagation
Stress range
Number of cycles
Types of details
  Flange cover plates
  Transverse stiffeners
  Bolted joints
  Longitudinal stiffeners

## Slide 55: Stress Range
Tension
Compression
Min.
Max.
Stress
Stress
Range
+
-
Stress
Tension
Compression
Min.
Stress
Max.
Stress
Stress
Range
+
-

## Slide 56: Flange Crack Growth Process
Rolled Beam
Cover Plate
Weld

## Slide 57: Through Crack at a Cover Plate

## Slide 58: Crack Propagation Into the Web

## Slide 59: Crack Growth at Transverse Stiffener Welded to Web
Stiffener
Web

## Slide 60: Constrained Induced Fracture (CIF)
Fracture is not due to fatigue or number of cycles
Occurs suddenly with no prior signs
Fractures are at intersecting welds or at small gaps between intersecting welds
Girder fracture at Hoan bridge Milwaukee was due to CIF

## Slide 61: Constraint Induced Fracture (CIF)
GUSSET
GIRDER
STIFFENER

## Slide 62: Constraint Induced Fracture (CIF)

## Slide 63: Constraint Induced Fracture (CIF)
Web Fracture

## Slide 64: Constraint Induced Fracture (CIF)
Transverse Stiffener
Longitudinal Stiffener
Web

## Slide 65: Inspection of Steel Members

## Slide 66: Inspection Procedures & Locations
Procedures
Visual
  Hands-on inspection
Physical
  Removal of dirt, paint etc.
Identification
  Fatigue crack may be identified by the development of rust stains
Advanced Inspection Techniques

## Slide 67
Locations
Bearing areas
Shear zones
Flexure zones
Fatigue prone details
Out-of-plane distortion
Constraint induced fracture detail
Secondary members
Areas that trap water and debris
Areas exposed to traffic
Inspection Procedures
& Locations

## Slide 68: Corroded Shear Zone & Diaphragm

## Slide 69: What to do if a Crack is Detected?
  Determine significance of crack on load carrying capacity
  Evaluate cause of cracking
  Show sketches with details of size and location
  Drill hole at the tip to arrest the growth
  Check with dye penetrant
  Take good photographs showing all the details
Note: Cracks perpendicular to primary stresses are very serious
Cracks parallel to primary stresses are less serious

## Slide 70: Inspection of Pin and Hanger

## Slide 71: Pin Location
70'
ABUT. #1
PIER #1
PIER #2
90'
HINGE
HINGE
90'
90'
70'
F.S.
45'
ABUT. #2

## Slide 72: Pin Detail
Pin
Shear Plates
Shear
Plates
Girder
Girder
Web
Bottom Flange

## Slide 73: Design Stresses in Pin
Nut
Pin

## Slide 74: Actual Stresses in Pin

## Slide 75: High Stress in Pin Due to Corrosion
Corrosion
Pin

## Slide 76: High Stress in Pin Due to Corrosion

## Slide 77: Hanger Location
ABUT. #1
PIER #1
PIER #2
114'
HANGER
170'
91'
ABUT. #2
HANGER
SUSPENDED SPAN
ANCHOR SPAN
ANCHOR SPAN

## Slide 78: Hanger Details
Suspended span
Anchor span

## Slide 79: Stresses in Hanger
Actual
Tension
Actual
Tension
Moment

## Slide 80: Deterioration of Pin & Hanger
Pin
  Frozen
  Corroded
  Cracks in welded shear plates
Hanger
  Twisted or bent
  Ceased
  Cracks in edges

## Slide 81: Inspection of Pins
Procedure
Determine if pins are functioning
Visual inspection not very effective
Ultrasonic inspection is required
Remove nuts if possible

## Slide 82: Pin Measurements
Bottom flange
elev. alignment
Bottom flange gap

## Slide 83: Preparation for Inspection

## Slide 84: Removal of Nuts

## Slide 85: U/T Inspection

## Slide 86: Inspection of Hangers
Procedure
Report any corrosion
Hanger plate is as critical as pin.
Examine edges
Check hangers for bowing, out of plane bending

## Slide 87: Measurements in Pin & Hanger
2
2
1
3
Suspended span

## Slide 88: Questions?